CATEGORY 2 - MATERIALS PROCESSING

2A	Systems, Equipment and Components

N.B.: 	For quiet running bearings, see ML9g.

2A001	Anti-friction bearings and bearing systems, as follows, and components therefor:

Note:	2A001 does not control balls with tolerances specified by the manufacturer in accordance with ISO 3290 as grade 5 or worse.

a.	Ball bearings and solid roller bearings having tolerances specified by the manufacturer in accordance with ABEC 7, ABEC 7P, ABEC 7T or ISO Standard Class 4 or better (or national equivalents), and having rings, balls or rollers made from monel or beryllium;

Note:	2A001.a. does not control tapered roller bearings.

b.	Other ball bearings and solid roller bearings having tolerances specified by the manufacturer in accordance with ABEC 9, ABEC 9P or ISO Standard Class 2 or better (or national equivalents);

Note:	2A001.b. does not control tapered roller bearings.

c.	Active magnetic bearing systems using any of the following:

1.	Materials with flux densities of 2.0 T or greater and yield strengths greater than 414 MPa;

2.	All-electromagnetic 3D homopolar bias designs for actuators; or

3.	High temperature (450 K (177°C) and above) position sensors.

2A225	Crucibles made of materials resistant to liquid actinide metals, as follows:

a.	Crucibles having both of the following characteristics:

1.	A volume of between 150 cm3 and 8,000 cm3; and

2.	Made of or coated with any of the following materials, having a purity of 98% or greater by weight:

a.	Calcium fluoride (CaF2);

b.	Calcium zirconate (metazirconate) (CaZrO3);

c.	Cerium sulphide (Ce2S3);

d.	Erbium oxide (erbia) (Er2O3);

e.	Hafnium oxide (hafnia) (HfO2);

f.	Magnesium oxide (MgO);

g.	Nitrided niobium-titanium-tungsten alloy (approximately 50% Nb, 30% Ti, 20% W);

h.	Yttrium oxide (yttria) (Y2O3); or

i.	Zirconium oxide (zirconia) (ZrO2);

b.	Crucibles having both of the following characteristics:

1.	A volume of between 50 cm3 and 2,000 cm3; and

2.	Made of or lined with tantalum, having a purity of 99.9% or greater by weight;

c.	Crucibles having all of the following characteristics:

1.	A volume of between 50 cm3 and 2,000 cm3;

2.	Made of or lined with tantalum, having a purity of 98% or greater by weight; and

3.	Coated with tantalum carbide, nitride, boride, or any combination thereof.

2A226	Valves having all of the following characteristics:

a.	A 'nominal size' of 5 mm or greater;

b.	Having a bellows seal; and

c.	Wholly made of or lined with aluminium, aluminium alloy, nickel, or nickel alloy containing more than 60% nickel by weight.

Technical Note:

For valves with different inlet and outlet diameters, the 'nominal size' in 2A226 refers to the smallest diameter.

2B	Test, Inspection and Production Equipment

Technical Notes:

1.	Secondary parallel contouring axes, (e.g., the w-axis on horizontal boring mills or a secondary rotary axis the centre line of which is parallel to the primary rotary axis) are not counted in the total number of contouring axes.

N.B.:	Rotary axes need not rotate over 360°.  A rotary axis can be driven by a linear device (e.g., a screw or a rack-and-pinion).

2.	Axis nomenclature shall be in accordance with International Standard ISO 841, 'Numerical Control Machines - Axis and Motion Nomenclature'.

3.	For the purposes of 2B001 to 2B009 a "tilting spindle" is counted as a rotary axis.

4.	Stated positioning accuracy levels derived from measurements made according to ISO 230/2 (1988)1 or national equivalents may be used for each machine tool model instead of individual machine tests.

N.B.:	Stated positioning accuracy means the accuracy value provided to the competent authorities of the Member State in which the exporter is established as representative of the accuracy of a machine model.

Determination of Stated Values

1.	Select five machines of a model to be evaluated;

2.	Measure the linear axis accuracies according to ISO 230/2 (1988) ;

3.	Determine the A-values for each axis of each machine. The method of calculating the A-value is described in the ISO standard;

4.	Determine the mean value of the A-value of each axis. This mean value Â becomes the stated value of each axis for the model (Âx    Ây...);

5.	Since the Category 2 list refers to each linear axis there will be as many stated values as there are linear axes;

6.	If any axis of a machine model not controlled by 2B001.a. to 2B001.c.or 2B201 has a stated accuracy Â of 6 microns for grinding machines and 8  microns for milling and turning machines or better, the manufacturer should be required to reaffirm the accuracy level once every eighteen months.

2B001	Machine tools, as follows, and any combination thereof, for removing (or cutting)

metals, ceramics or "composites", which, according to the manufacturer’s technical specification, can be equipped with electronic devices for "numerical control":

N.B.:	SEE ALSO 2B201.

a.	Machine tools for turning, having all of the following characteristics:

1.	Positioning accuracy with "all compensations available" equal to or less (better) than 6 µm according to ISO 230/2 (1988) or national equivalents along any linear axis ; and

2.	Two or more axes which can be coordinated simultaneously for "contouring control";

Note:	2B001.a. does not control turning machines specially designed for the production of contact lenses.

b.	Machine tools for milling, having any of the following characteristics:

1.	a.	Positioning accuracy with "all compensations available" equal to or less (better) than 6 µm according to ISO 230/2 (1988)2 or national equivalents along any linear axis; and

b.	Three linear axes plus one rotary axis which can be coordinated simultaneously for "contouring control";

2.	Five or more axes which can be coordinated simultaneously for "contouring control"; or

3.	A positioning accuracy for jig boring machines, with "all compensations available", equal to or less (better) than 4 µm according to ISO 230/2 (1988)2 or national equivalents along any linear axis;

c.	Machine tools for grinding, having any of the following characteristics:

1.	a.	Positioning accuracy with "all compensations available" equal to or less (better) than 4 µm according to ISO 230/2 (1988) or national equivalents along any linear axis; and

b.	Three or more axes which can be coordinated simultaneously for "contouring control"; or

2.	Five or more axes which can be coordinated simultaneously for "contouring control";

Note:	2B001.c. does not control grinding machines, as follows:

1.	Cylindrical external, internal, and external-internal grinding machines having all the following characteristics:

a.	Limited to cylindrical grinding; and

b.	Limited to a maximum workpiece capacity of 150 mm outside diameter or length.

2.	Machines designed specifically as jig grinders having any of the following characteristics:

a.	The c-axis is used to maintain the grinding wheel normal to the work surface; or

b.	The a-axis is configured to grind barrel cams.

3.	Tool or cutter grinding machines limited to the production of tools or cutters.

4.	Crank shaft or cam shaft grinding machines.

5.	Surface grinders.

d.	Electrical discharge machines (EDM) of the non-wire type which have two or

more rotary axes which can be coordinated simultaneously for "contouring control";

e.	Machine tools for removing metals, ceramics or "composites":

1.	By means of:

a.	Water or other liquid jets, including those employing abrasive additives;

b.	Electron beam; or

c.	"Laser" beam; and

2.	Having two or more rotary axes which:

a.	Can be coordinated simultaneously for "contouring control"; and

b.	Have a positioning accuracy of less (better) than 0.003°;

f.	Deep-hole-drilling machines and turning machines modified for deep-hole-drilling, having a maximum depth-of-bore capability exceeding 5,000 mm and specially designed components therefor.

2B003	"Numerically controlled" or manual machine tools, and specially designed

components, controls and accessories therefor, specially designed for the shaving, finishing, grinding or honing of hardened (Rc = 40 or more) spur, helical and double-helical gears with a pitch diameter exceeding 1,250 mm and a face width of 15% of pitch diameter or larger finished to a quality of AGMA 14 or better (equivalent to ISO 1328 class 3).

2B004	Hot "isostatic presses", having all of the following, and specially designed components

and accessories therefor:

N.B.:	SEE ALSO 2B104 and 2B204.

a.	A controlled thermal environment within the closed cavity and a chamber cavity with an inside diameter of 406 mm or more; and

b.	Any of the following:

1.	A maximum working pressure exceeding 207 MPa;

2.	A controlled thermal environment exceeding 1,773 K (1,500°C); or

3.	A facility for hydrocarbon impregnation and removal of resultant gaseous degradation products.

Technical Note:

The inside chamber dimension is that of the chamber in which both the working temperature and the working pressure are achieved and does not include fixtures. That dimension will be the smaller of either the inside diameter of the pressure chamber or the inside diameter of the insulated furnace chamber, depending on which of the two chambers is located inside the other.

N.B.	For specially designed dies, moulds and tooling see 1B003, 9B009 and the Military Goods Controls.

2B005	Equipment specially designed for the deposition, processing and in-process control of

inorganic overlays, coatings and surface modifications, as follows, for non-electronic substrates, by processes shown in the Table and associated Notes following 2E003.f., and specially designed automated handling, positioning, manipulation and control components therefor:

a.	"Stored programme controlled" chemical vapour deposition (CVD) production equipment having all of the following:

1.	Process modified for one of the following:

a.	Pulsating CVD;

b.	Controlled nucleation thermal deposition (CNTD); or

c.	Plasma enhanced or plasma assisted CVD; and

2.	Any of the following:

a.	Incorporating high vacuum (equal to or less than 0.01 Pa) rotating seals; or

b.	Incorporating in situ  coating thickness control;

b.	"Stored programme controlled" ion implantation production equipment having beam currents of 5 mA or more;

c.	"Stored programme controlled" electron beam physical vapour deposition (EB-PVD) production equipment incorporating power systems rated for over 80 kW, having any of the following:

1.	A liquid pool level "laser" control system which regulates precisely the ingots feed rate; or

2.	A computer controlled rate monitor operating on the principle of photo-luminescence of the ionised atoms in the evaporant stream to control the deposition rate of a coating containing two or more elements;

d.	"Stored programme controlled" plasma spraying production equipment having any of the following characteristics:

1.	Operating at reduced pressure controlled atmosphere (equal to or less than 10 kPa measured above and within 300 mm of the gun nozzle exit) in a vacuum chamber capable of evacuation down to 0.01 Pa prior to the spraying process; or

2.	Incorporating in situ  coating thickness control;

e.	"Stored programme controlled" sputter deposition production equipment capable of current densities of 0.1 mA/mm2 or higher at a deposition rate of 15 µm/h or more;

f.	"Stored programme controlled" cathodic arc deposition production equipment incorporating a grid of electromagnets for steering control of the arc spot on the cathode;

g.	"Stored programme controlled" ion plating production equipment allowing for the in situ measurement of any of the following:

1.	Coating thickness on the substrate and rate control; or

2.	Optical characteristics.

Note:	2B005 does not control chemical vapour deposition, cathodic arc, sputter deposition, ion plating or ion implantation equipment specially designed for cutting or machining tools.

2B006	Dimensional inspection or measuring systems and equipment, as follows:

a.	Computer controlled, "numerically controlled" or "stored programme controlled" dimensional inspection machines, having a three dimensional length (volumetric) "measurement uncertainty" equal to or less (better) than (1.7 + L/1,000) µm (L is the measured length in mm) tested according to ISO 10360-2;

N.B.:	SEE ALSO 2B206.

b.	Linear and angular displacement measuring instruments, as follows:

1.	Linear measuring instruments having any of the following:

a.	Non-contact type measuring systems with a "resolution" equal to or less (better) than 0.2 µm within a measuring range up to 0.2 mm;

b.	Linear voltage differential transformer systems having all of the following characteristics:

1.	"Linearity" equal to or less (better) than 0.1% within a measuring range up to 5 mm; and

2.	Drift equal to or less (better) than 0.1% per day at a standard ambient test room temperature ±1 K; or

c.	Measuring systems having all of the following:

1.	Containing a "laser"; and

2.	Maintaining, for at least 12 hours, over a temperature range of ±1 K around a standard temperature and at a standard pressure, all of the following:

a.	A "resolution" over their full scale of 0.1 µm or less (better); and

b.	A "measurement uncertainty" equal to or less (better) than (0.2 + L/2,000) µm (L is the measured length in mm);

Note:	2B006.b.1. does not control measuring interferometer systems, without closed or open loop feedback, containing a "laser" to measure slide movement errors of machine-tools, dimensional inspection machines or similar equipment.

2.	Angular measuring instruments having an "angular position deviation" equal to or less (better) than 0.00025°;

Note:	2B006.b.2. does not control optical instruments, such as autocollimators, using collimated light to detect angular displacement of a mirror.

c.	Equipment for measuring surface irregularities, by measuring optical scatter as a function of angle, with a sensitivity of 0.5 nm or less (better).

Note 1:	Machine tools which can be used as measuring machines are controlled if they meet or exceed the criteria specified for the machine tool function or the measuring machine function.

Note 2:	A machine described in 2B006 is controlled if it exceeds the control threshold anywhere within its operating range.

2B007	"Robots" having any of the following characteristics and specially designed controllers

and "end-effectors" therefor:

N.B.:	SEE ALSO 2B207.

a.	Capable in real time of full three-dimensional image processing or full three-dimensional 'scene analysis' to generate or modify "programmes" or to generate or modify numerical programme data;

Note:	The 'scene analysis' limitation does not include approximation of the third dimension by viewing at a given angle, or limited grey scale interpretation for the perception of depth or texture for the approved tasks (2 1/2 D).

b.	Specially designed to comply with national safety standards applicable to explosive munitions environments;

c.	Specially designed or rated as radiation-hardened to withstand a total radiation dose greater than 5 x 103 Gy (silicon) without operational degradation; or

Technical Note:

The term Gy(silicon) refers to the energy in Joules per kilogram absorbed by an unshielded silicon sample when exposed to ionising radiation.

d.	Specially designed to operate at altitudes exceeding 30,000 m.

2B008	Assemblies, units or inserts specially designed for machine tools or for equipment

specified in 2B006 or 2B007, as follows:

a.	Linear position feedback units (e.g., inductive type devices, graduated scales, infrared systems or "laser" systems) having an overall "accuracy" less (better) than (800 + (600 x L x 10-3)) nm (L equals the effective length in mm);

Note:	For "laser" systems see also Note to 2B006.b.1.

b.	Rotary position feedback units (e.g., inductive type devices, graduated scales, infrared systems or "laser" systems) having an "accuracy" less (better) than 0.00025°;

Note:	For "laser" systems see also Note to 2B006.b.1.

c.	"Compound rotary tables" and "tilting spindles", capable of upgrading, according to the manufacturer's specifications, machine tools to or above the levels specified in 2B.

2B009	Spin-forming machines and flow-forming machines, which, according to the

manufacturer's technical specification, can be equipped with "numerical control"

units or a computer control and having all of the following:

N.B.:	SEE ALSO 2B109 AND 2B209.

a.	Two or more controlled axes of which at least two can be coordinated simultaneously for "contouring control"; and

b.	A roller force more than 60 kN.

Technical Note:

Machines combining the function of spin-forming and flow-forming are for the purpose of 2B009 regarded as flow-forming machines.

2B104	Equipment and process controls designed or modified for densification and

pyrolysis of structural composite rocket nozzles and reentry vehicle nose tips.

Note:	The only "isostatic presses" and furnaces specified in 2B104 are as follows:

a.	"Isostatic presses", other than those specified in 2B004, having all the following characteristics:

1.	Maximum working pressure of 69 MPa or greater;

2.	Designed to achieve and maintain a controlled thermal environment of 873 K (600oC) or greater; and;

3.	Possessing a chamber cavity with an inside diameter of 254 mm or greater; ;

b.	CVD Furnaces designed or modified for the densification of carbon-carbon composites.

2B109	Flow-forming machines, other than those specified in 2B009, and specially designed

components therefor, which:

N.B.:	SEE ALSO 2B209.

a.	According to the manufacturer's technical specification, can be equipped with "numerical control" units or a computer control, even when not equipped with such units; and

b.	With more than two axes which can be coordinated simultaneously for "contouring control".

Technical Notes:

1.	Machines combining the function of spin-forming and flow-forming are for the purpose of 2B109  regarded as flow-forming machines.

2.	2B109 does not control machines that are not usable in the production of propulsion components and equipment (e.g. motor cases) for systems specified in 9A005, 9A007.a. or 9A105.a.

2B116	Vibration test systems, equipment and components therefor, as follows:

a.	Vibration test systems employing feedback or closed loop techniques and incorporating a digital controller, capable of vibrating a system at 10 g rms or more over the entire range 20 Hz to 2,000 Hz and imparting forces of 50 kN, measured 'bare table', or greater;

b.	Digital controllers, combined with specially designed vibration test software, with a "real-time bandwidth" greater than 5 kHz  designed for use with vibration test systems specified in 2B116.a.;

c.	Vibration thrusters (shaker units), with or without associated amplifiers, capable of imparting a force of 50 kN, measured 'bare table', or greater and usable in vibration test systems specified in 2B116.a.;

d.	Test piece support structures and electronic units designed to combine multiple shaker units in a system capable of providing an effective combined force of 50 kN, measured 'bare table', or greater, and usable in vibration systems specified in 2B116.a.

Note:	In 2B116, 'bare table' means a flat table, or surface, with no fixture or fittings.

2B201	Machine tools, other than those specified in 2B001, as follows, for removing or cutting

metals, ceramics or "composites", which, according to the manufacturer’s technical specification, can be equipped with electronic devices for simultaneous "contouring control" in two or more axes:

a.	Machine tools for milling, having any of the following characteristics:

1.	Positioning accuracies with "all compensations available" equal to or less (better) than 6 µm according to ISO 230/2 (1988) or national equivalents along any linear axis; or

2.	Two or more contouring rotary axes;

Note:	2B201.a. does not control milling machines having the following characteristics:

a.	X-axis travel greater than 2 m; and

b.	Overall positioning accuracy on the x-axis more (worse) than 30 µm.

b.	Machine tools for grinding, having any of the following characteristics:

1.	Positioning accuracies with "all compensations available" equal to or less (better) than 4 µm according to ISO 230/2 (1988)4 or national equivalents along any linear axis; or

2.	Two or more contouring rotary axes.

Note:	2B201.b. does not control the following grinding machines:

a.	Cylindrical external, internal, and external-internal grinding  machines having all of the following characteristics:

1.	Limited to cylindrical grinding;

2.	A maximum workpiece outside diameter or length of 150 mm;

3.	Not more than two axes that can be coordinated simultaneously for "contouring control"; and

4.	No contouring c axis;

b.	Jig grinders with axes limited to x, y, c and a where c axis is used to maintain the grinding wheel normal to the work surface, and the a axis is configured to grind barrel cams;

c.	Tool or cutter grinding machines with "software" specially designed for the production of tools or cutters; or

d.	Crankshaft or camshaft grinding machines.

2B204 	"Isostatic presses", other than those specified in 2B004 or 2B104, and related equipment, as follows:

a.	"Isostatic presses" having both of the following characteristics:

1.	Capable of achieving a maximum working pressure of 69 MPa or greater; and

2.	A chamber cavity with an inside diameter in excess of 152 mm;

b.	Dies, moulds and controls, specially designed for "isostatic presses" specified in  2B204.a.

Technical Note:

In 2B204 the inside chamber dimension is that of the chamber in which both the working temperature and the working pressure are achieved and does not include fixtures. That dimension will be the smaller of either the inside diameter of the pressure chamber or the inside diameter of the insulated furnace chamber, depending on which of the two chambers is located inside the other.

2B206	Dimensional inspection machines, instruments or systems, other than those specified

in 2B006, as follows:

a.	Computer controlled or numericaly controlled dimensional inspection machines having both of the following characteristics:

1.	Two or more axes; and

2.	A one-dimensional length "measurement uncertainty" equal to or less (better) than (1.25 + L/1000) µm tested with a probe of an "accuracy" of less (better) than 0.2 µm (L is the measured length in millimeters) (Ref.:VDI/VDE 2617 Parts 1 and 2);

b.	Systems for simultaneously linear-angular inspection of hemishells, having both of the following characteristics:

1.	"Measurement uncertainty" along any linear axis equal to or less (better) than 3.5 µm per 5 mm; and

2.	"Angular position deviation" equal to or less than 0.02°.

Note 1:	Machine tools that can be used as measuring machines are controlled if they meet or exceed the criteria specified for the machine tool function or the measuring machine function.

Note 2:	A machine specified in 2B206 is controlled if it exceeds the control threshold anywhere within its operating range.

Technical Notes:

1.	The probe used in determining the measurement uncertainty of a dimensional inspection system shall be described in VDI/VDE 2617 parts 2, 3 and 4.

2.	All parameters of measurement values in 2B206 represent plus/minus i.e., not total band.

2B207	"Robots", "end-effectors" and control units, other than those specified in 2B007, as

follows:

a.	"Robots" or "end-effectors" specially designed to comply with national safety standards applicable to handling high explosives (for example, meeting electrical code ratings for high explosives);

b.	Control units specially designed for any of the "robots" or "end-effectors" specified in 2B207.a.

2B209	Flow forming machines, spin forming machines capable of flow forming functions,

other than those specified in 2B009 or 2B109, and mandrels, as follows:

a.	Machines having both of the following characteristics:

1.	Three or more rollers (active or guiding); and

2.	Which, according to the manufacturer's technical specification, can be equipped with "numerical control" units or a computer control;

b.	Rotor-forming mandrels designed to form cylindrical rotors of inside diameter between 75 mm and 400 mm.

Note:	2B209.a. includes machines which have only a single roller designed to deform metal plus two auxiliary rollers which support the mandrel, but do not participate directly in the deformation process.

2B225	Remote manipulators that can be used to provide remote actions in radiochemical

separation operations or hot cells, having either of the following characteristics:

a.	A capability of penetrating 0.6 m or more of hot cell wall (through-the-wall operation); or

b.	A capability of bridging over the top of a hot cell wall with a thickness of 0.6 m or more (over-the-wall operation).

Techncial Note:

Remote manipulators provide translation of human operator actions to a remote operating arm and terminal fixture. They may be of 'master/slave' type or operated by joystick or keypad.

2B226	Controlled atmosphere (vacuum or inert gas) induction furnaces, and power supplies

therefor, as follows:

N.B:	SEE ALSO 3B.

a.	Furnaces having all of the following characteristics:

1.	Capable of operation above 1,123 K (850°C);

2.	Induction coils 600 mm or less in diameter; and

3.	Designed for power inputs of 5 kW or more;

b.	Power supplies, with a specified power output of 5 kW or more, specially designed for furnaces specified in 2B226.a.

Note:	2B226.a. does not control furnaces designed for the processing of semiconductor wafers.

2B227	Vacuum or other controlled atmosphere metallurgical melting and casting furnaces

and related equipment, as follows:

a.	Arc remelt and casting furnaces having both of the following characteristics:

1.	Consumable electrode capacities between 1,000 cm3 and 20,000 cm3, and

2.	Capable of operating with melting temperatures above 1,973 K (1,700oC);

b.	Electron beam melting furnaces and plasma atomization and melting furnaces, having both of the following characteristics:

1.	A power of 50 kW or greater; and

2.	Capable of operating with melting temperatures above 1,473 K (1,200oC).

c.	Computer control and monitoring systems specially configured for any of the furnaces specified in 2B227.a. or b.

2B228	Rotor fabrication or assembly equipment, rotor straightening equipment,

bellows-forming mandrels and dies, as follows:

a.	Rotor assembly equipment for assembly of gas centrifuge rotor tube sections, baffles, and end caps;

Note:	2B228.a. includes precision mandrels, clamps, and shrink fit machines.

b.	Rotor straightening equipment for alignment of gas centrifuge rotor tube sections to a common axis;

Technical Note:

In 2B228.b. such equipment normally consists of precision measuring probes linked to a computer that subsequently controls the action of, for example, pneumatic rams used for aligning the rotor tube sections.

c.	Bellows-forming mandrels and dies for producing single-convolution bellows.

Technical Note:

In 2B228.c. the bellows have all of the following characteristics:

1.	Inside diameter between 75 mm and 400 mm;

2.	Length equal to or greater than 12.7 mm;

3.	Single convolution depth greater than 2 mm; and

4.	Made of high-strength aluminium alloys, maraging steel or high strength "fibrous or filamentary materials".

2B229	Centrifugal multiplane balancing machines, fixed or portable, horizontal or vertical,

as follows:

a.	Centrifugal balancing machines designed for balancing flexible rotors having a length of 600 mm or more and having all of the following characteristics:

1.	Swing or journal diameter greater than 75 mm;

2.	Mass capability of from 0.9 to 23 kg ; and

3.	Capable of balancing speed of revolution greater than 5,000 r.p.m.;

b.	Centrifugal balancing machines designed for balancing hollow cylindrical rotor components and having all of the following characteristics:

1.	Journal diameter greater than 75 mm;

2.	Mass capability of from 0.9 to 23 kg;

3.	Capable of balancing to a residual imbalance equal to or less than  0.01 kg x mm/kg per plane; and

4.	Belt drive type.

2B230	"Pressure transducers" capable of measuring absolute pressures at any point in the

range 0 to 13 kPa and having both of the following characteristics:

a.	Pressure sensing elements made of or protected by aluminium, aluminium alloy, nickel or nickel alloy with more than 60% nickel by weight; and

b.	Having either of the following characteristics:

1.	A full scale of less than 13 kPa and an 'accuracy' of better than + 1% of full-scale; or

2.	A full scale of 13 kPa or greater and an 'accuracy' of better than  + 130 Pa.

Technical Note:

For the purposes of 2B230, 'accuracy' includes non-linearity, hysteresis and repeatability at ambient temperature.

2B231	Vacuum pumps having all of the following characteristics:

a.	Input throat size equal to or greater than 380 mm;

b.	Pumping speed equal to or greater than 15 m3/s; and

c.	Capable of producing an ultimate vacuum better than 13 mPa.

Technical Notes:

1.	The pumping speed is determined at the measurement point with nitrogen gas or air.

2.	The ultimate vacuum is determined at the input of the pump with the input of the pump blocked off.

2B232	Multistage light gas guns or other high-velocity gun systems (coil, electromagnetic,

and electrothermal types, and other advanced systems) capable of accelerating projectiles to 2 km/s or greater.

2B350	Chemical manufacturing facilities and equipment, as follows:

a.	Reaction vessels or reactors, with or without agitators, with total internal (geometric) volume greater than 0.1 m3 (100 litres) and less than 20 m3 (20,000 litres), where all surfaces that come in direct contact with the chemical(s) being processed or contained are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Fluoropolymers;

3.	Glass (including vitrified or enamelled coating or glass lining);

4.	Nickel or alloys with more than 40% nickel by weight;

5.	Tantalum or tantalum alloys;

6.	Titanium or titanium alloys; or

7.	Zirconium or zirconium alloys;

b.	Agitators for use in reaction vessels or reactors where all surfaces of the agitator that come in direct contact with the chemical(s) being processed or contained are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Fluoropolymers;

3.	Glass (including vitrified or enamelled coatings or glass lining);

4.	Nickel or alloys with more than 40% nickel by weight;

5.	Tantalum or tantalum alloys;

6.	Titanium or titanium alloys; or

7.	Zirconium or zirconium alloys;

c.	Storage tanks, containers or receivers with a total internal (geometric) volume greater than 0.1 m3 (100 litres) where all surfaces that come in direct contact with the chemical(s) being processed or contained are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Fluoropolymers;

3.	Glass (including vitrified or enamelled coatings or glass lining);

4.	Nickel or alloys with more than 40% nickel by weight;

5.	Tantalum or tantalum alloys;

6.	Titanium or titanium alloys; or

7.	Zirconium or zirconium alloys;

d.	Heat exchangers or condensers with a heat transfer surface area of less than 20 m2, where all surfaces that come in direct contact with the chemical(s) being processed are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Fluoropolymers;

3.	Glass (including vitrified or enamelled coatings or glass lining);

4.	Graphite;

5.	Nickel or alloys with more than 40% nickel by weight;

6.	Tantalum or tantalum alloys;

7.	Titanium or titanium alloys; or

8.	Zirconium or zirconium alloys;

e.	Distillation or absorption columns of internal diameter greater than 0.1 m, where all surfaces that come in direct contact with the chemical(s) being processed are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Fluoropolymers;

3.	Glass (including vitrified or enamelled coatings or glass lining);

4.	Graphite;

5.	Nickel or alloys with more than 40% nickel by weight;

6.	Tantalum or tantalum alloys;

7.	Titanium or titanium alloys; or

8.	Zirconium or zirconium alloys;

f.	Remotely operated filling equipment in which all surfaces that come in direct contact with the chemical(s) being processed are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight; or

2.	Nickel or alloys with more than 40% nickel by weight;

g.	Multiple seal valves incorporating a leak detection port, bellows-seal valves, non-return (check) valves or diaphragm valves, in which all surfaces that come in direct contact with the chemical(s) being processed or contained are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Fluoropolymers;

3.	Glass (including vitrified or enamelled coatings or glass lining);

4.	Nickel or alloys with more than 40% nickel by weight;

5.	Tantalum or tantalum alloys;

6.	Titanium or titanium alloys; or

7.	Zirconium or zirconium alloys;

h.	Multi-walled piping incorporating a leak detection port, in which all surfaces that come in direct contact with the chemical(s) being processed or contained are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Fluoropolymers;

3.	Glass (including vitrified or enamelled coatings or glass lining);

4.	Graphite;

5.	Nickel or alloys with more than 40% nickel by weight;

6.	Tantalum or tantalum alloys;

7.	Titanium or titanium alloys; or

8.	Zirconium or zirconium alloys;

i.	Multiple-seal, canned drive, magnetic drive, bellows or diaphragm pumps, with manufacturer's specified maximum flow-rate greater than 0.6 m3/hour, or vacuum pumps with manufacturer's specified maximum flow-rate greater than 5 m3/hour (under standard temperature (273 K (0oC)) and pressure (101.3 kPa) conditions), in which all surfaces that come in direct contact with the chemical(s) being processed are made from any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Ceramics;

3.	Ferrosilicon;

4.	Fluoropolymers;

5.	Glass (including vitrified or enamelled coatings or glass lining);

6.	Graphite;

7.	Nickel or alloys with more than 40% nickel by weight;

8.	Tantalum or tantalum alloys;

9.	Titanium or titanium alloys; or

10.	Zirconium or zirconium alloys;

j.	Incinerators designed to destroy chemicals specified in entry 1C350, having specially designed waste supply systems, special handling facilities and an average combustion chamber temperature greater than 1,273 K (1,000oC), in which all surfaces in the waste supply system that come into direct contact with the waste products are made from or lined with any of the following materials:

1.	Alloys with more than 25% nickel and 20% chromium by weight;

2.	Ceramics; or

3.	Nickel or alloys with more than 40% nickel by weight.

2B351	Toxic gas monitoring systems, as follows; and dedicated detectors therefor:

a.	Designed for continuous operation and usable for the detection of chemical warfare agents or chemicals specified in 1C350, at concentrations of less than 0.3 mg/m3; or

b.	Designed for the detection of cholinesterase-inhibiting activity.

2B352	Equipment capable of use in handling biological materials, as follows:

a.	Complete biological containment facilities at P3, P4 containment level;

Technical Note:

P3 or P4 (BL3, BL4, L3, L4) containment levels are as specified in the WHO Laboratory Biosafety manual (Geneva, 1983).

b.	Fermenters capable of cultivation of pathogenic “microorganisms”, viruses or capable of toxin production, without the propagation of aerosols, and having a total capacity of 100 litres or more;

Technical Note:

Fermenters include bioreactors, chemostats and continuous-flow systems.

c.	Centrifugal separators, capable of continuous separation without the propagation of aerosols, having all the following characteristics:

1.	Flow rate exceeding 100 litres per hour;

2.	Components of polished stainless steel or titanium;

3.	Double or multiple sealing joints within the steam containment area; and

4.	Capable of in-situ steam sterilisation in a closed state;

Technical Note:

Centrifugal separators include decanters.

d.	Cross-flow filtration equipment, capable of continuous separation without the propagation of aerosols, having both of the following characteristics:

1.	Equal to or greater than 5 m2; and

2.	Capable of in-situ sterilization;

e.	Steam sterilisable freeze drying equipment with a condenser capacity exceeding 50 kg of ice in 24 hours and less than 1,000 kg of ice in 24 hours;

f.	Equipment that incorporates or is contained in P3 or P4 containment housing, as follows:

1.	Independently ventilated protective full or half suits;

2.	Class III biological safety cabinets or isolators with similar performance standards;

Note:	In 2B352.f.2., isolators include flexible isolators, dry boxes, anaerobic chambers, glove boxes and laminar flow hoods.

g.	Chambers designed for aerosol challenge testing with "microorganisms" or "toxins" and having a capacity of 1 m3 or greater.

2C	Materials

None.

2D	Software

2D001	"Software", other than that specified in 2D002, specially designed or modified for

the "development", "production" or "use" of equipment specified in 2A001or

2B001 to 2B009.

2D002	"Software" for electronic devices, even when residing in an electronic device or

system, enabling such devices or systems to function as a "numerical control" unit, capable of any of the following:

a.	Coordinating simultaneously more than four axes for "contouring control"; or

b.	"Real time processing" of data to modify tool path, feed rate and spindle data, during the machining operation, by any of the following:

1.	Automatic calculation and modification of part program data for machining in two or more axes by means of measuring cycles and access to source data; or

2.	"Adaptive control" with more than one physical variable measured and processed by means of a computing model (strategy) to change one or more machining instructions to optimize the process.

Note:	2D002 does not control "software" specially designed or modified for the operation of machine tools not controlled by Category 2.

2D101	"Software" specially designed for the "use" of equipment specified in 2B104, 2B109

or 2B116.

N.B.:	SEE ALSO 9D004.

2D201	"Software" specially designed for the "use" of equipment specified in 2B204, 2B206,

2B207, 2B209, 2B227 or 2B229.

2D202	"Software" specially designed or modified for the "development", "production" or "use"

of equipment specified in 2B201.

2E	Technology

2E001	"Technology" according to the General Technology Note for the "development" of

equipment or "software" specified in 2A, 2B or 2D.

2E002	“Technology" according to the General Technology Note for the "production" of

equipment specified in 2A or 2B.

2E003	Other "technology", as follows:

a.	"Technology" for the "development" of interactive graphics as an integrated part in "numerical control" units for preparation or modification of part programmes;

b.	"Technology" for metal-working manufacturing processes, as follows:

1.	"Technology" for the design of tools, dies or fixtures specially designed for any of the following processes:

a.	"Superplastic forming";

b.	"Diffusion bonding"; or

c.	"Direct-acting hydraulic pressing";

2.	Technical data consisting of process methods or parameters as listed below used to control:

a.	"Superplastic forming" of aluminium alloys, titanium alloys or "superalloys":

1.	Surface preparation;

2.	Strain rate;

3.	Temperature;

4.	Pressure;

b.	"Diffusion bonding" of "superalloys" or titanium alloys:

1.	Surface preparation;

2.	Temperature;

3.	Pressure;

c.	"Direct-acting hydraulic pressing" of aluminium alloys or titanium alloys:

1.	Pressure;

2.	Cycle time;

d.	"Hot isostatic densification" of titanium alloys, aluminium alloys or "superalloys":

1.	Temperature;

2.	Pressure;

3.	Cycle time;

c.	"Technology" for the "development" or "production" of hydraulic stretch-forming machines and dies therefor, for the manufacture of airframe structures;

d.	"Technology" for the "development" of generators of machine tool instructions (e.g., part programmes) from design data residing inside "numerical control" units;

e.	"Technology" for the "development" of integration "software" for incorporation of expert systems for advanced decision support of shop floor operations into "numerical control" units;

f.	"Technology" for the application of inorganic overlay coatings or inorganic surface modification coatings (specified in column 3 of the following table) to non-electronic substrates (specified in column 2 of the following table), by processes specified in column 1 of the following table and defined in the Technical Note.

Note:	The table and Technical Note appear after entry 2E391.

2E101	"Technology" according to the General Technology Note for the "use" of equipment or

"software" specified in 2B004, 2B104, 2B109, 2B116 or 2D101.

2E201	"Technology" according to the General Technology Note for the "use" of equipment or

"software" specified in 2A225, 2A226, 2B001, 2B006, 2B007.b., 2B007.c., 2B008, 2B009, 2B201, 2B204, 2B206, 2B207, 2B209, 2B225 to 2B232, 2D201 or 2D202.

2E301	"Technology" according to the General Technology Note for the "use" of goods specified in 2B350 to 2B352.

2E390	Process "technology", including licences, designed for the manufacture of chemical

[A]	weapons agents or their precursors, and/or for their disposal, or for whole plants

designed for their manufacture

2E391	“Technology”, including licences, designed for the manufacture of equipment

[A]	specified in 2B350 and 2B351.

# TABLE - DEPOSITION TECHNIQUES

1.	Coating Process (1)*	2.	Substrate	3.	Resultant Coating

A.	Chemical Vapour		"Superalloys" 		Aluminides for internal

Deposition  (CVD)				passages

Ceramics (19) and Low-		Silicides

expansion glasses (14)		Carbides

Dielectric layers (15)

Diamond

Diamond-like carbon (17)

Carbon-carbon,		Silicides

Ceramic and		Carbides

Metal "matrix"		Refractory metals

"composites"		Mixtures thereof (4)

Dielectric layers (15)

Aluminides

Alloyed aluminides (2)

Boron nitride

Cemented tungsten		Carbides

carbide (16),		Tungsten

Silicon carbide (18)		Mixtures thereof (4)

Dielectric layers (15)

Molybdenum and		Dielectric layers (15)

Molybdenum alloys

Beryllium and		Dielectric layers (15)

Beryllium alloys		Diamond

Diamond-like carbon (17)

# TABLE - DEPOSITION TECHNIQUES

1.	Coating Process (1)*	2.	Substrate	3.	Resultant Coating

A.	Chemical Vapour		Sensor window		Dielectric layers (15)

Deposition  (CVD)		materials (9)		Diamond

(continued)				Diamond-like carbon (17)

B.	Thermal-Evaporation

Physical Vapour

Deposition (TE-PVD)

B.1.	Physical Vapour		"Superalloys"		Alloyed silicides

Deposition (PVD):				Alloyed aluminides (2)

Electron-Beam				MCrAlX (5)

(EB-PVD)				Modified zirconia (12)

Silicides

Aluminides

Mixtures thereof (4)

Ceramics (19) and Low-		Dielectric layers (15)

expansion glasses (14)

Corrosion resistant		MCrAlX (5)

steel (7)		Modified zirconia (12)

Mixtures thereof (4)

Carbon-carbon,		Silicides

Ceramic and		Carbides

Metal "matrix"		Refractory metals

"composites"		Mixtures thereof (4)

Dielectric layers (15)

Boron nitride

Cemented tungsten		Carbides

carbide (16),		Tungsten

Silicon carbide (18)		Mixtures thereof (4)

Dielectric layers (15)

Molybdenum and		Dielectric layers (15)

Molybdenum alloys

Beryllium and		Dielectric layers (15)

Beryllium alloys		Borides

Beryllium

Sensor window		Dielectric layers (15)

materials (9)

Titanium alloys (13)		Borides

Nitrides

# TABLE - DEPOSITION TECHNIQUES

1.	Coating Process (1)*	2.	Substrate	3.	Resultant Coating

B.2.	Ion assisted resistive		Ceramics (19) and Low-		Dielectric layers (15)

heating Physical Vapour		expansion glasses (14)		Diamond-like carbon (17)

Deposition (PVD)

(Ion Plating)

Carbon-carbon,		Dielectric layers (15)

Ceramic and Metal

"matrix" "composites"

Cemented tungsten		Dielectric layers (15)

carbide (16),

Silicon carbide

Molybdenum and

Molybdenum alloys		Dielectric layers (15)

Beryllium and

Beryllium alloys		Dielectric layers (15)

Sensor window		Dielectric layers (15)

materials (9)		Diamond-like carbon (17)

B.3.	Physical Vapour		Ceramics (19) and Low-		Silicides

Deposition (PVD):		expansion glasses (14)		Dielectric layers (15)

"Laser" Vaporization				Diamond-like carbon (17)

Carbon-carbon,		Dielectric layers (15)

Ceramic and Metal

"matrix" "composites"

Cemented tungsten		Dielectric layers (15)

carbide (16),

Silicon carbide

Molybdenum and		Dielectric layers (15)

Molybdenum alloys

Beryllium and		Dielectric layers (15)

Beryllium alloys

Sensor window		Dielectric layers (15)

materials (9)		Diamond-like carbon

B.4.	Physical Vapour		"Superalloys"		Alloyed silicides

Deposition (PVD):				Alloyed aluminides (2)

Cathodic Arc Discharge				MCrAlX (5)

Polymers (11) and		Borides

Organic "matrix"		Carbides

"composites"		Nitrides

Diamond-like carbon (17)

# TABLE - DEPOSITION TECHNIQUES

1.	Coating Process (1)*	2.	Substrate	3.	Resultant Coating

C.	Pack cementation		Carbon-carbon,		Silicides

(see A above for		Ceramic and		Carbides

out-of-pack		Metal "matrix"		Mixtures thereof (4)

cementation) (10)		"composites"

Titanium alloys (13)		Silicides

Aluminides

Alloyed aluminides (2)

Refractory metals		Silicides

and alloys (8)		Oxides

D.	Plasma spraying		"Superalloys"		MCrAlX (5)

Modified zirconia (12)

Mixtures thereof (4)

Abradable Nickel-Graphite

Abradable materials

containing Ni-Cr-Al

Abradable Al-Si-Polyester

Alloyed aluminides (2)

Aluminium alloys (6)		MCrAlX (5)

Modified zirconia (12)

Silicides

Mixtures thereof (4)

Refractory metals		Aluminides

and alloys (8)		Silicides

Carbides

Corrosion resistant		MCrAlX (5)

steel (7)		Modified zirconia (12)

Mixtures thereof (4)

Titanium alloys (13)		Carbides

Aluminides

Silicides

Alloyed aluminides (2)

Abradable Nickel-Graphite

Abradable materials

containing Ni-Cr-Al

Abradable Al-Si-Polyester

E.	Slurry Deposition 		Refractory metals		Fused silicides

and alloys (8)		Fused aluminides

except for resistance

heating elements

Carbon-carbon,		Silicides

Ceramic and		Carbides

Metal "matrix"		Mixtures thereof (4)

"composites"

# TABLE - DEPOSITION TECHNIQUES

1.	Coating Process (1)*	2.	Substrate	3.	Resultant Coating

F.	Sputter Deposition 		"Superalloys"		Alloyed silicides

Alloyed aluminides (2)

Noble metal modified

aluminides (3)

MCrAlX (5)

Modified zirconia (12)

Platinum

Mixtures thereof (4)

Ceramics and Low-		Silicides

expansion glasses (14)		Platinum

Mixtures thereof (4)

Dielectic layers (15)

Diamond-like carbon (17)

Titanium alloys (13)		Borides

Nitrides

Oxides

Silicides

Aluminides

Alloyed aluminides (2)

Carbides

Carbon-carbon,		Silicides

Ceramic and Metal		Carbides

"matrix" "composites"		Refractory metals

Mixtures thereof (4)

Dielectric layers (15)

Boron nitride

Cemented tungsten		Carbides

carbide (16),		Tungsten

Silicon carbide (18)		Mixtures thereof (4)

Dielectric layers (15)

Boron nitride

Molybdenum and

Molybdenum alloys		Dielectric layers (15)

Beryllium and		Borides

Beryllium alloys		Dielectric layers (15)

Beryllium

Sensor window		Dielectric layers (15)

materials (9)		Diamond-like carbon (17)

Refractory metals		Aluminides

and alloys (8)		Silicides

Oxides

Carbides

# TABLE - DEPOSITION TECHNIQUES

1.	Coating Process (1)*	2.	Substrate	3.	Resultant Coating

G.	Ion Implantation 		High temperature		Additions of

bearing steels		Chromium

Tantalum or

Niobium (Columbium)

Titanium alloys (13)		Borides

Nitrides

Beryllium and		Borides

Beryllium alloys

Cemented tungsten		Carbides

carbide (16)		Nitrides

## TABLE - DEPOSITION TECHNIQUES - NOTES

1.	The term 'coating process' includes coating repair and refurbishing as well as original coating.

2.	The term 'alloyed aluminide coating' includes single or multiple-step coatings in which an element or elements are deposited prior to or during application of the aluminide coating, even if these elements are deposited by another coating process. It does not, however, include the multiple use of single-step pack cementation processes to achieve alloyed aluminides.

3.	The term 'noble metal modified aluminide' coating includes multiple-step coatings in which the noble metal or noble metals are laid down by some other coating process prior to application of the aluminide coating.

4.	The term 'mixtures thereof' includes infiltrated material, graded compositions, co-deposits and multilayer deposits and are obtained by one or more of the coating processes specified in the Table.

5.	'MCrAlX' refers to a coating alloy where M equals cobalt, iron, nickel or combinations thereof and X equals hafnium, yttrium, silicon, tantalum in any amount or other intentional additions over 0.01 weight percent in various proportions and combinations, except:

a.	CoCrAlY coatings which contain less than 22 weight percent of chromium, less than 7 weight percent of aluminium and less than 2 weight percent of yttrium;

b.	CoCrAlY coatings which contain 22 to 24 weight percent of chromium, 10 to 12 weight percent of aluminium and 0.5 to 0.7 weight percent of yttrium; or

c.	NiCrAlY coatings which contain 21 to 23 weight percent of chromium, 10 to 12 weight percent of aluminium and 0.9 to1.1 weight percent of yttrium.

6.	The term 'aluminium alloys' refers to alloys having an ultimate tensile strength of 190 MPa or more measured at 293 K (20°C).

7.	The term 'corrosion resistant steel' refers to AISI (American Iron and Steel Institute) 300 series or equivalent national standard steels.

8.	'Refractory metals and alloys' include the following metals and their alloys: niobium (columbium), molybdenum, tungsten and tantalum.

9.	'Sensor window materials', as follows: alumina, silicon, germanium, zinc sulphide, zinc selenide, gallium arsenide, diamond, gallium phosphide, sapphire and the following metal halides: sensor window materials of more than 40 mm diameter for zirconium fluoride and hafnium fluoride.

10.	"Technology" for single-step pack cementation of solid airfoils is not controlled by Category 2.

11.	'Polymers', as follows: polyimide, polyester, polysulphide, polycarbonates and polyurethanes.

12.	'Modified zirconia' refers to additions of other metal oxides (e.g., calcia, magnesia, yttria, hafnia, rare earth oxides) to zirconia in order to stabilise certain crystallographic phases and phase compositions.  Thermal barrier coatings made of zirconia, modified with calcia or magnesia by mixing or fusion, are not controlled.

13.	'Titanium alloys' refers only to aerospace alloys having an ultimate tensile strength of 900 MPa or more measured at 293 K (20°C).

14.	'Low-expansion glasses' refers to glasses which have a coefficient of thermal expansion of 1 x 10-7 K-1 or less measured at 293 K (20°C).

15.	'Dielectric layers' are coatings constructed of multi-layers of insulator materials in which the interference properties of a design composed of materials of various refractive indices are used to reflect, transmit or absorb various wavelength bands. Dielectric layers refers to more than four dielectric layers or dielectric/metal "composite" layers.

16.	'Cemented tungsten carbide' does not include cutting and forming tool materials consisting of tungsten carbide/(cobalt, nickel), titanium carbide/(cobalt, nickel), chromium carbide/nickel-chromium and chromium carbide/nickel.

17.	"Technology" specially designed to deposit diamond-like carbon on any of the following is not controlled:

magnetic disk drives and heads, polycarbonate eyeglasses, equipment for the manufacture of disposables, bakery equipment, valves for faucets, acoustic diaphragms for speakers, engine parts for automobiles, cutting tools, punching-pressing dies, high quality lenses designed for cameras or telescopes, office automation equipment, microphones or medical devices.

18.	'Silicon carbide' does not include cutting and forming tool materials.

19.	Ceramic substrates, as used in this entry, does not include ceramic materials containing 5% by weight, or greater, clay or cement content, either as separate constituents or in combination.

## TABLE - DEPOSITION TECHNIQUES - TECHNICAL NOTE

Processes specified in Column 1 of the Table are defined as follows:

a.	Chemical Vapour Deposition (CVD) is an overlay coating or surface modification coating process wherein a metal, alloy, "composite", dielectric or ceramic is deposited upon a heated substrate.  Gaseous reactants are decomposed or combined in the vicinity of a substrate resulting in the deposition of the desired elemental, alloy or compound material on the substrate.  Energy for this decomposition or chemical reaction process may be provided by the heat of the substrate, a glow discharge plasma, or "laser" irradiation.

N.B.1	CVD includes the following processes: directed gas flow out-of-pack deposition, pulsating CVD, controlled nucleation thermal deposition (CNTD), plasma enhanced or plasma assisted CVD processes.

N.B.2	Pack denotes a substrate immersed in a powder mixture.

N.B.3	The gaseous reactants used in the out-of-pack process are produced using the same basic reactions and parameters as the pack cementation process, except that the substrate to be coated is not in contact with the powder mixture.

b.	Thermal Evaporation-Physical Vapour Deposition (TE-PVD) is an overlay coating process conducted in a vacuum with a pressure less than 0.1 Pa wherein a source of thermal energy is used to vaporize the coating material.  This process results in the condensation, or deposition, of the evaporated species onto appropriately positioned substrates.

The addition of gases to the vacuum chamber during the coating process to synthesize compound coatings is an ordinary modification of the process.

The use of ion or electron beams, or plasma, to activate or assist the coating's deposition is also a common modification in this technique.  The use of monitors to provide in-process measurement of optical characteristics and thickness of coatings can be a feature of these processes.

Specific TE-PVD processes are as follows:

1.	Electron Beam PVD uses an electron beam to heat and evaporate the material which forms the coating;

2.	Ion Assisted Resistive Heating PVD employs electrically resistive heating sources in combination with impinging ion beam(s) to produce a controlled and uniform flux of evaporated coating species;

3.	"Laser" Vaporization uses either pulsed or continuous wave "laser" beams to vaporize the material which forms the coating;

4.	Cathodic Arc Deposition employs a consumable cathode of the material which forms the coating and has an arc discharge established on the surface by a momentary contact of a ground trigger.  Controlled motion of arcing erodes the cathode surface creating a highly ionized plasma.  The anode can be either a cone attached to the periphery of the cathode, through an insulator, or the chamber.  Substrate biasing is used for non line-of-sight deposition.

N.B.	This definition does not include random cathodic arc deposition with non-biased substrates.

5.	Ion Plating is a special modification of a general TE-PVD process in which a plasma or an ion source is used to ionize the species to be deposited, and a negative bias is applied to the substrate in order to facilitate the extraction of the species from the plasma.  The introduction of reactive species, evaporation of solids within the process chamber, and the use of monitors to provide in-process measurement of optical characteristics and thicknesses of coatings are ordinary modifications of the process.

c.	Pack Cementation is a surface modification coating or overlay coating process wherein a substrate is immersed in a powder mixture (a pack), that consists of:

1.	The metallic powders that are to be deposited (usually aluminium, chromium, silicon or combinations thereof);

2.	An activator (normally a halide salt); and

3.	An inert powder, most frequently alumina.

The substrate and powder mixture is contained within a retort which is heated to between 1,030 K (757°C) and 1,375 K (1,102°C) for sufficient time to deposit the coating.

d.	Plasma Spraying is an overlay coating process wherein a gun (spray torch) which produces and controls a plasma accepts powder or wire coating materials, melts them and propels them towards a substrate, whereon an integrally bonded coating is formed.  Plasma spraying constitutes either low pressure plasma spraying or high velocity plasma spraying.

N.B.1	Low pressure means less than ambient atmospheric pressure.

N.B.2	High velocity refers to nozzle-exit gas velocity exceeding 750 m/s calculated at 293 K (20°C) at 0.1 MPa.

e.	Slurry Deposition is a surface modification coating or overlay coating process wherein a metallic or ceramic powder with an organic binder is suspended in a liquid and is applied to a substrate by either spraying, dipping or painting, subsequent air or oven drying, and heat treatment to obtain the desired coating.

f.	Sputter Deposition is an overlay coating process based on a momentum transfer phenomenon, wherein positive ions are accelerated by an electric field towards the surface of a target (coating material).  The kinetic energy of the impacting ions is sufficient to cause target surface atoms to be released and deposited on an appropriately positioned substrate.

N.B.1	The Table refers only to triode, magnetron or reactive sputter deposition which is used to increase adhesion of the coating and rate of deposition and to radio frequency (RF) augmented sputter deposition used to permit vaporisation of non-metallic coating materials.

N.B.2	Low-energy ion beams (less than 5 keV) can be used to activate the deposition.

- Ion Implantation is a surface modification coating process in which the element to be alloyed is ionized, accelerated through a potential gradient and implanted into the surface region of the substrate.  This includes processes in which ion implantation is performed simultaneously with electron beam physical vapour deposition or sputter deposition.

This page intentionally blank

Manufacturers calculating positioning accuracy in accordance with ISO 230/2 (1997) should consult the Australian Department of Defence.

Manufacturers calculating positioning accuracy in accordance with ISO 230/2 (1997) should consult the Australian Department of Defence.

Manufacturers calculating positioning accuracy in accordance with ISO 230/2 (1997) should consult the Australian Department of Defence.

Manufacturers calculating positioning accuracy in accordance with ISO 230/2 (1997) should consult the Australian Department of Defence.

*	 	The numbers in parenthesis refer to the Notes following this Table.

*	 	The numbers in parenthesis refer to the Notes following this Table.

*	 	The numbers in parenthesis refer to the Notes following this Table.

*	 	The numbers in parenthesis refer to the Notes following this Table.

*	 	The numbers in parenthesis refer to the Notes following this Table.

*	 	The numbers in parenthesis refer to the Notes following this Table.